Type 2.B

Type 2.B – Paragraph Form

Product shall be ECTC Type 2.B, which is comprised of natural and/or polymer fibers mechanically interlocked and/or chemically adhered together to form a netless RECP. Product shall have a C Factor ≤ 0.10 from standardized large‐scale rainfall performance testing, ASTM D6459 or equivalent deemed acceptable by the engineer. Product unvegetated permissible shear stress rating shall be ≥ 1.0 lbs/ft2 (≥48 Pa) according to ASTM D6460 or equivalent deemed acceptable by the engineer. MD (Machine Direction) tensile strength shall be ≥ 125 lbs/ft (≥ 1.8 kN/m) x TD (Transverse Direction) tensile strength of ≥ 10 lbs/ft (≥ 0.1 kN/m) according to ASTM D6818. Product shall have a thickness ≥ 0.3 in (≥ 7.6 mm) according to ASTM D6525, ground coverage of ≥ 50% - ≤ 90% according to ASTM D6567, and mass per unit area of ≥ 10.0 oz/yd2 (≥ 339 g/m2) according to ASTM D6475.

Type 2.B – Tabular Form

|  |  |
| --- | --- |
| ECTC Type | 2.B |
| Product Description | Netless Rolled Erosion Control Blankets |
| Material Composition | Natural and/or polymer fibers mechanically interlocked and/or chemically adhered together to form a netless RECP |
| C Factorb | ≤ 0.10 |
| Shear Stressc | ≥ 1.0 lbs/ft2 (≥ 48 Pa) |
| MD Material Tensile Strength(ASTM D6818) | ≥ 125 lbs/ft (≥ 1.8 kN/m) |
| TD Material Tensile Strength(ASTM D6818) | ≥ 10 lbs/ft (≥ 0.1 kN/m) |
| Material Thickness (ASTM D6525) | ≥ 0.30 in (≥ 7.6 mm) |
| Ground Coverage (ASTM D6567) | ≥ 50% - ≤ 90% |
| Mass Per Unit Area (ASTM D6475) | ≥ 10.0 oz/yd2 (≥ 339 g/m2) |

*a. C Factor and permissible shear stress for Types 1.A. and 2.A. mulch control nettings must be obtained with netting used in conjunction with pre‐applied mulch material.*

*b. ASTM D6459 or equivalent deemed acceptable by the engineer.*

*c. ASTM D6460 or equivalent deemed acceptable by the engineer.*